## Slide 1: Experience with resistive coatings at Saclay
and Carleton, Nikhef, Neuchatel
Use of resistive coatings for:
Spreading the charge to improve resolution while limiting the number of electronic readout channels
Stabilizing Micromegas detectors (spark suppression)
Protecting integrated circuits
Numerous techniques tried since a decade
Characterization of coverlays : measurement of surface resistivity, bulk resistivity and thru-resistivity
P. Colas

## Slide 2: ILC-TPC : charge spreading
Resistive bulk Micromegas
Continuous RC circuit spreads the charge -> resolution improvement
60 µ resolution at 0 drift with 3 mm pads !

## Slide 3
Argon/Isobutane 90/10
Cr (SiO2)n cermet
P.C., M. Dixit, I. Giomataris
2005 LC workshop, Stanford
Also the resistive foil stabilizes Micromegas: no more breakdown, stable current

## Slide 4
Standard Micromegas
Resistive Micromegas
MAMMA beam test, 15 kHz hadron beam, October 2009

## Slide 5
Resistive deposits also protect TimePix Chips from sparks
(10 microns of aSi:H, 4-7 microns of SixNy (H. VdGraaf, N. Wyrsch)

## Slide 7
Deposition of thin layers (10 µ thick) of a-SiH (1013 W.cm)
Neuchatel, N. Wyrsch
Possibility to add a doped layer on top

## Slide 8
lxL resistive sample = L/l ’squares’
Conducting tape, insulating substrate
Measure resistance, divide by number of squares
4-point probe (Neuchatel)
Circular probe
We used several techniques to measure resistivities.
May depend on voltage, pressure of the contact,…
Often see discrepancies, inhomogeneities, unstabilities
Thru-resistivity sometimes inconsistent with surface resistivity

## Slide 9
Diagnostic tools : thermal image of the prototype with a high-resistivity layer and a lower-resistivity layer on top (N. Wyrsch, EPFL, Neuchatel)
Hot spots due to leakage current

## Slide 10
Type of coating | PROs | CONs
Cermet (Sheldal; M. Dixit et al.) | Tunable resistivity, homogeneous Stable once laminated | Fragile / scratchable
Carbon-Loaded polyimide (Dupont; M. Dixit et al.) | Accurate thickness (25 µ) Large surfaces easy | 
Thin layer deposition (H. VdGraaf, N. Wyrsch, EPFL) | Limited to few micron thickness | Limited to small surfaces (10x10cm2). Very clean substrate needed.
Sprays (G. Mikenberg, Tel Aviv, J. Répond, I.Laktineh) | Large surfaces. Needs tuning | 10-20% homogeneity
paints | Can be patterned. Large surfaces. | inhomogeneous