## Slide 1: RD51Collaboration meeting 13/04/2011
Resistors in Cern PCB worshop

## Slide 2: Summary
Terminology
Materials and techniques
Structures made at CERN

## Slide 3: Terminilogy
-A Resistor is define by:
-Value Ohms
-Precision %
-TCR ppm/Deg C
-max power W or W/m2
-breakdown voltage V
-Resistivity in Ohm*m
-Sheet resistance or surface resistivity in Ohm/sqr
-TCR: Temperature coefficient of the resistor
-Cermet: is a composite material composed of ceramic (cer) and metallic (met) materials.

## Slide 4: Rs: Sheet resistance Ω/sq
Source: Wikipedia

## Slide 5: Some examples
@ 300 K(Ω·m)
  Silver 16·10-9 (Ω·m)
  Ruthenium 71 10-9 (Ω·m)
  Germanium 460·10-9 (Ω·m)
  Ni/Cr 1000·10-9 (Ω·m)
  Carbone 35 000·10-9 (Ω·m)

## Slide 6: Resistor families
Thin-film :Vacuum deposited metals/oxides
Thick-film : (Cer-met)
Polymer (epoxy, phenolic, polyimide)

## Slide 7: Thin film

## Slide 8: Thin film
WEB SITE: http://www.ohmega.com

## Slide 9: Thick film
Some supplier can build 100 Mohms/sqr pastes

## Slide 10: Polymer resistive pastes
1 Mohms/Sqr seems to be the limit for these polymers

## Slide 11: Polymer Resistive foils

## Slide 12: Other products

## Slide 13: Selection guide
Substrate
  Thin film
    Mineral materials: Ceramic, glass, silicon, metals
    Polymers
  Thick film
    Mineral materials: Ceramic, glass, silicon, metals
  Polymers
    All type

## Slide 14: Selection guide
-High values
  Thick-film on ceramic (up to 1-10 GOhms/sqr)
  Thin-film on polymer (antistatic material 10G-100GOhms/sqr)
  Polymer patterned layers
-Precision
  Thick film on ceramic (up to 1 GOhms/sqr)
  Thin film low values (up to 100kOhms/sqr)
-Large size
  Polymers
  Thin-film on polymers

## Slide 15: Full Resistive I
Substrate PCB or Ceramic
-Type:
Thin film
Thick film
Resistive polymer
-Deposit:
Vacuum deposit*
Painting
Screen printing
Spraying*
* Not made at CERN

## Slide 16
Copper
Dielectric: polymer or ceramic
PCB or ceramic
Resistive layer (all types)
Pads for read out
200mm x 150mm
Bulk Micromegas with
Full Resistive layer
Full Resistive Ii

## Slide 17: Patterned resistive layer
PCB
PCB
PCB
PCB
All resistor type but needs:
-photolithography
-and/or Wet etch
-and/or laser ablation

## Slide 18: Thick and plated
PCB
Only Polymer resistors
-Thicknesses up to 200um
-Silver based glues for the top

## Slide 19: Embedded
75um
Copper strip
Resistor
Pad
Microvia
- All Resistors types

## Slide 20: Resistive strip I
PCB
PCB
PCB
All resistor type but needs:
-photolithography
-and/or Wet etch
-and/or laser ablation

## Slide 21: Resistive strip II
Copper Strip
Resistive Strip
Dielectric 0.1mm
Active area up to 1m
PCB
Cross section
PCB

## Slide 22: Resistive strip III
PCB
Resistive Strip
Copper Strip
GND
Embedded resistor

## Slide 23: Thank you