## Slide 1: Beam test of Linear Collider TPC Micromegas module with fully integrated electronics
* D. Attié, A. Bellerive, P. Colas, E. Delagnes, M. Dixit, I. Giamatoris, P. Hayman, J.-P. Martin, M. Riallot, N. Shiell, Y-H Shin and W. Wang (Saclay, Carleton, Montreal, TRIUMF)
Tracking & Vertexing 27 Sept 2011, LCWS11 Granada
Madhu Dixit
Carleton University & TRIUMF
On behalf of LC TPC collaboration Micromegas group*

## Slide 2: Outline
The Time Projection Chamber for the Linear Collider
Micro Pattern Gas Detector options for ILD TPC readout:
  Standard GEM readout
  Micromegas with charge dispersion, a new MPGD readout concept
1 meter Large Prototype TPC (LP TPC) development & tests at DESY to establish the design parameters for the ILD-TPC
Summary of LP TPC tests with a single Micromegas module (2008-2010) to measure single hit transverse resolution, TPC readout electronics adapted from T2K TPCs
LP TPC first results with the first of 7+2 (spare) Micromegas modules:
  To measure & demonstrate momentum resolution performance
  To address integration issues, serial production and characterization, multimodule issues (alignment, distortions)
Summary

## Slide 3: The TPC central tracker for the Linear Collider
The ILD detector concept plans to use a ~2.2 meter drift TPC read out with Micro Pattern Gas Detectors
Unprecedented transverse resolution goals driven by model independent Higgs measurements limited only by the precision of collision energy
Measure 200 track points
r,  ≤ 100 m (stiff radial tracks, full drift distance)
z ≈ 500 - 1500 m (zero to full drift)
Double hit resolution:
≈ 2mm in (r,)
≈ 6 mm in z
dE/dx ~ 5%
Conventional wire/pad TPC limited by intrinsic ExB effects

## Slide 4
3-5 mm
~ 100 µm
Signal too narrow for conventional Micromegas for good resolution with 1 mm wide pads
GEM resolution ok ~ 1 mm wide pads
Micro-Pattern Gas Detector (MPGD) readout for Linear Collider TPC

## Slide 5: Micro-Pattern Gas Detector Options for ILD TPC Readout
For the GEM, increased transverse diffusion in the transfer & induction gaps provides a natural mechanism to disperse avalanche charge facilitating pad centroid determination from charge sharing
The conventional GEM readout would use narrow ~1 mm wide pads to achieve the 100 µm ILD TPC resolution goal
The Micromegas exploits the concept of charge dispersion in Micro Pattern Gas Detectors with a resistive anode and can use wider pads to achieve the ILD resolution goal
A resolution of 50 µm at zero drift distance has been achieved with ~3 mm wide pads for the charge dispersion Micromegas TPC readout option
MPGDs have no preferred track angle & negligible ExB effect

## Slide 6: Charge dispersion in a MPGD with a resistive anode
Concept first proven for the GEM. Modified anode with a high resistivity film bonded to a readout plane with an insulating spacer.
2-dimensional continuous RC network defined by material properties & geometry.
Point charge at r=0 & t=0 disperses with time.
Time dependent charge dispersion on anode facilitates precision pad centroid determination.
Equation for anode surface charge density function on the 2D continuous RC network:
(r,t) integral over pads
(r)
Q
r / mm
mm
ns

## Slide 7: Large Prototype LP TPC - EUDET Test Facility at DESY
SiPM Cosmic
Trigger Setup
LP : part of a
TPC endplate
PCMAG: superconducting solenoid, B = 1.2T
e- test beam at DESY
(1GeV/c<p<6GeV/c)
Translation stage

## Slide 8: LP TPC tests with a single Micromegas module (2008-10)
Resistive ink
~3 MΩ/□
Resistive Kapton
~5 MΩ/□
Standard
Resistive Kapton
~3 MΩ/□
Bulk Micromegas: pillars hold the mesh on the whole surface: no need for frame
Resistive bulk: continuous 2D RC network to disperse the charge
The LP TPC was outfitted & tested with different Micromegas modules (one at a time) to compare performance

## Slide 9: Micromegas LP TPC readout module pad layout
Z=20cm, 200 ns shaping
Relative fraction of ‘charge’ seen by the pad, vs x(pad)-x(track)
24 rows x 72 columns 3 x 6.8 mm² pads
0

## Slide 10
Z=5cm
Z=35cm
Z=50cm
MEAN RESIDUAL vs ROW number
Z-independent distortions
Distortions up to 50 microns for resistive ink (blue points)
RMS 7 microns for CLK film (red points)
Track position dependent bias due to non-uniformities in anode film resistivity and readout structure assembly
Carbon loaded Kapton is much more uniform than resistive ink

## Slide 11
Response to cosmic rays & beam particles
Average charge by row
Using cosmic-ray events
B=OT
Excellent uniformity up to the edge of the readout module for the ‘bulk’ Micromegas technology.
Average charge by row
Using 5 GeV electrons
B=1T
0 5 10 15 20
0 5 10 15 20
z distribution

## Slide 12
Module 4
Single hit transverse resolution measurement (B = 0T & 1T)
Carbon-loaded Kapton (~5 MΩ/□)
B=0 T Cd = 315.1 µm/√cm (Magboltz)
Module 3
B=1 T Cd = 94.2 µm/√cm (Magboltz)
χ2/Ndof = 10.6/10
χ2/Ndof = 29.1/11
Average of B=0T data and B=1T data
  Neff = 38.0±0.2(stat) ±0.8 (Cd syst)
  σ0= 59 ± 3 µm

## Slide 13
180 kHz (5 x 2 cm² beam) showed no charging effects and stable operation
Peaking time ~300 ns sufficient to distinguish 2 tracks on the same pad
4µs
Time (in 40 ns bins)
Test in a high intensity pion beam at CERN (July 2010)

## Slide 14
Toward 7+2 module project and electronics integration

## Slide 15: Beam test of first Micromegas module with integrated electronics - May 2011
New detector: new routing to adapt to new connectors, lower anode resistivity (3 MΩ/□), new resistive film, grounding on the edge of the PCB.
New 300 points flat connectors
New front end: keep naked AFTER chips and remove double diodes (depend on resistive film to protect against sparks)
New Front End Mezzanine (FEM)
New backend ready for up to 12 modules
New DAQ, 7-module ready and more compact format
New trigger discriminator and logic (FPGA)

## Slide 16: Integrated electronics for 7-module project
Remove packaging and protection diodes
Wire –bond AFTER chips
Use 2 × 300 pins connector
Use tiniest resistors (1 mm × 0.5 mm) from O to 10W
25 cm
14 cm
0,78 cm
0,74 cm
4,5 cm
12,5 cm
2,8 cm
3,5 cm
3,5 cm
FEC
Chip
After 2 weeks of operation: no ASIC lost. The resistive film protects against sparks.

## Slide 17: First prototype of electronics readout board

## Slide 18
New Micromegas module with integrated electronics

## Slide 19: Toward 7 Module Analysis with Marlin Integration
Existing single module software was ported from Fortran and is incompatible with Marlin
Progress to date:
Converted most anonymous namespaces to classes (named remaining namespaces)
Ensured classes have only relevant functions
Moved main function out of library
Turned separate PRF, BIAS, & DD analysis code into proper subclasses selected based on command-line user input
Removed all errors revealed by compiling with -Wall
Organized files into proper “include” and “source” files
Begin to implement proper C++ coding practices
Further work to be done:
    Marlin consistent co-ordinate system
    Multihit capability
    Implement version control (SVN)
    Check for any classes/functions that are already implemented in Marlin
    Modify front end of code to be consistent with Marlin “Processes”
    Apply Marlin coding standards (including cmake)

## Slide 20: A new Pad Response Function (PRF)
Existing 4 parameter PRF (ratio of two symmetric quartics) replaced with a simpler one:
Only two parameters
Easier to work with
Better fits to data
(mm)

## Slide 21: Bias before and after bias calibration
With no external silicon tracker information the accuracy of bias calibration, determined from internal consistency of TPC data, is statistically limited
Bias before
Bias after ~ 20 µm

## Slide 22
Preliminary results of new module beam test (B=1T)
May 2011
Transverse resolution dependence on peaking time

## Slide 23: Short peaking time preferable for timing & two track resolution
Small Z => Better resolution for shorter peaking time
Large Z => Better resolution for longer peaking time
However, we get:=>
Work in progress: Reintegrate short peaking time signal for good resolution at all Z

## Slide 24: SUMMARY
A baseline Micromegas module for LP TPC is now well defined
A module with fully integrated electronics has been tested in a beam. Resolution ~ 50µm for 3mm wide pads
Seven module analysis software development in progress
A serial production and characterization will be carried out in 2012. A test bench at CERN will be used to study the uniformity and thermal properties

## Slide 25
Spare slides

## Slide 26: Abstract
The Micromegas option for the ILD TPC readout exploits the new concept of charge dispersion in Micro Pattern Gas Detectors with a resistive anode. The Large Prototype TPC (LP TPC) beam tests done so far with a single Micromegas module have demonstrated that the requisite single hit transverse resolution can be achieved. Toward demonstrating the ILD TPC momentum resolution goal, the LP TPC was outfitted and tested earlier this year at DESY with the first of seven Micromegas modules to be built with on-board integrated electronics. The present status of development & results from the beam test will be presented.

## Slide 28: Old PRF – Ratio of two symmetric quartics