## Slide 1: The LHC Upgrades in Luminosity and Energy: Options and Plan
Lucio Rossi
CERN
High Lumi LHC Coordinator
CEA Saclay – IRFU/SPP 17 September2012

## Slide 2: Highlights
LHC today : performance
Luminosity : which goal, parameters and hardware changes
High Luminosity LHC
  Magnets
  SC Crab Cavities
  SC Links
LHC: a long history, a longer future?
High Energy: towards a farther energy frontier

## Slide 3: LHC: the numbers
27 km, p-p at 7+7 TeV 3.5+3.5 start, 4+4 in 2012
1232 x 15 m Twin Dipoles
Operational field 8.3 T @11.85 kA (9 T design)
HEII cooling, 1.9 K with 3 km circuits (130 tonnes He inventory).
Field homogeneity of 10-4 at 1 cm from the coils, bending strength uniformity better then 10-3. Field quality control (geometric and SC effects) at 10-5.

## Slide 4: LHC: the numbers (cont.)
392 Main Quads Two-In-One rated for a peak field of 7 T.
About 100 other Two-in-One MQs
32 MQX (low-) single bore for luminosity (design L=11034 cm-2s-1), 70 mm apertures, about 8 T peak field, high quality
A «zoo» of 7600 «small» Sc magnets (correctors and higher order magnets, till dodecapoles: so far only 6th and 8-th pole used)
Total: 9 MJ stored energy (at nominal)
Large detector magnets
  ATLAS toroid – 25 m long 1.2 MJ
  CMS solenois – 12 m long 2.5 MJ

## Slide 5: LHC: the numbers (cont.)
400 MHz Standing wave RF
4 single cell cavities in cryomodule, 2 crym per beam. Total 16 cavities.
Sputtered niobium design (as LEP)
Gradient 5.5 MV/m nominal (8 MV/m available)
Nominal 2MV, up to 3 MV at 8 MV/m
Center frequency mechanically tunable in a range of 100kHz by a stepper motor
Located in P4 (es LEP experiment) share cryo with the magnets

## Slide 6
At less than 1% of nominal intensity LHC enters new territory. Collimators must survive expected beam loss…
The power of LHC beams
Nominal LHC design: 3 × 1014 protons accelerated to 7 TeV/c
circulating at 11 kHz in a SC ring
LHC today

## Slide 7: Performance
Equiv 7 TeV
Typical 2012.
Luminosity:  rate of collisions
Best period 3 weeks in June !!
77: New record Aug

## Slide 8: Performance (cont.)
Promised minimum 2011 : 1 fb-1
Promised 2012 (after extension) : 25 fb-1
Integrated lumi:  # of collisions
Higgs got!

## Slide 9: Higgs found

## Slide 10: From here: where to go? The CERN 10 y plan

## Slide 11: Next ten year plan for LHC
Shut down to fix interconnects and overcome energy limitation (LHC incident of Sept 2008)
Shut down to overcome beam intensity limitation (Injectors, collimation)

## Slide 12: Luminosity: main ingredients
energy
Beam current
Beam size
Beam current and emittance: involve Inj chain and whole ring
β involve «only» 2 IRs, 600 m.
Unit of lumi through the talk
LHC has been designed for L0 All systems have singularly designed tentatively for ultimate 2L0 (to be verified…)

## Slide 13: High Luminosity LHC project
To push the performance above the ultimate, to 5 1034 or more
  If pile up allows it. Today we have 30-35, experiments design upgrade for 140 evt/crossing average with a max of 200/crossing)
  If energy deposition by collision debris in the nearest SC magnets (low. triplet quads) allows it
Use of lumi levelling to maximize integrated luminosity for a given max lumi.
Final goal is : 3000 fb-1 by 10-12 years

## Slide 14: Target parameters for HL-LHC run
Efficiency is defined as the ratio between the annual luminosity target of 250 fb-1 over the potential luminosity that can be reached with an ideal cycle run time with no stop for 150 days: trun= tlev+tdec+tturn. The turnaround time after a beam dump is taken as 5 hours, tdecay is 3 h while tlev depends on the total beam current
baseline

## Slide 15: Cycle in the HL-LHC run
20E+34
pile up
heat deposition in IR and DS
other?
Levelling

## Slide 16: Pushing virtual lumi up to make longer run
25 ns
w/o
leveling
25 ns
leveled
virtual
peak
luminosity
tlev
tdec
tta
t [h]
L [1034 cm-2s-1]
50 ns leveled

## Slide 17: The goal 3000 fb-1 in 10-12 years

## Slide 18: Here the magnets for the low  in present LHC

## Slide 19: Changing 300x2 m both ATLAS & CMS (+LHC-b & Alice …)
1.2 km of LHC !!

## Slide 20: HL-LHC installation all around the ring…
6.5 kW@4.5K cryoplant
2 x 18 kW @4.5K cryoplants for IRs

## Slide 21
US LARP: Magnet Develop. Chart
G.L. Sabbi , LBNL

## Slide 22
LARP (US LHC program) Magnets
SQ
SM
TQS
LR
LQS-4m
HQ
TQC

## Slide 23: Results LARP LQ (90 mm vs 70 mm LHC)
LHC equivalent today
G. Ambrosio, FNAL

## Slide 24: LARP HQ (120 mm- 13 T)
S. Caspi , LBNL

## Slide 25: Improved Nb-Ti technology Low- quads and MS magnets
new insulation scheme, more porous in the coils and in the structure
Higher heat removal (matching the gap to NbSn ?)

## Slide 26: Avoid off-momentum protons on SC dipoles (diffractive)
5.5 m Nb3Sn
5.5 m Nb3Sn
3.5 m Collim.
5.5 m Nb3Sn
3.5 m Collim
5.5 m Nb3Sn

## Slide 27: Warm collimators in the cold region
A. Bertarelli of the EN-MME team

## Slide 28: Cold collimator design
D. Duarte Ramos
Ch. Mucher
External actuation system
Cold mass
Jaw cooling hose (from E-line)
Cu/W Collimator jaws with embedded cooling pipe
He heater (from 55K to >80K)

## Slide 29: 11 T-11 m dipole CERN-FNAL collaborations
Series to LHC dipoles: BL/I =120Tm/11.85kA
  Cable, strand constrained
  Nested power supply 300 A
Field quality
  Fe saturation 6.50.5
  Pers. Current (40 m fil. Size): 44 2010? Enough (few magnet)
Forces, energy 70% higher in same envelope
Demo (single, 2 m) by 2012; Proto by 2013-14
1 unit = 2x5.5mstraight
First NbSn in operation?
LHC
11 T

## Slide 30: 11 T Demo 2 m single bore
Project launched September 2010
Fermilab/CERN collaboration
Collared coil Dec 2011
Cold mass finished in May 2012
Test: very good to 10.4 T
Limited by a single spot
Next model by beginning of 2013

## Slide 31: Performance targets for Nb3Sn
JC (kA/mm2)
Dfil (m)
RRR (-)
Performance
Peak field
Cost
Stability Protection
Magnetization Field Quality
Stability
2.5
2
1.5
3
3.5
1
4
200
150
100
50
10
20
50
100
PIT
RRP
target
Target performance:
Jc > 3 kA/mm2
Dfil < 20 m
RRR > 100

## Slide 32: Procured strands
Work is on-going on a new strand architecture (169 stack) to reduce the filament diameter to 52 mm at 1 mm strand diameter, and 35 mm at 0.7 mm strand diameter
R&D started for an alternative architecture with filaments of 30 mm at 0.7 mm strand diameter
0.7 mm, 108/127 stack RRP from Oxford OST
1 mm, 192 tubes PIT from Bruker EAS

## Slide 33: Material R&D (basic science)
By courtesy of I. Pong and L. Oberli
Strand center
Coarse grains
Fine grains

## Slide 34: The successful SMC-3 cable
1.25 mm PIT strand, 14 strands
Conductor: done? Not at all: instability and FQ issues will continue to play a major role
Strand, cabling and cable behavior need to be modelized more deeply.

## Slide 35: Crab Cavity, for p-beam rotation at fs level!

## Slide 36: Effect of the crab cavity
RF crab cavity deflects head and tail in opposite direction so that collision is effectively “head on” and then luminosity is maximized
Crab cavity maximzes the lumi and can be used also for lumimosity levelling: if the lumi is too high, initially you don’t use it, so lumi is reduced by the geometrical factor. Then they are slowly turned on to compensate the proton burning

## Slide 37: Crab Cavity:
Effort going on at SLAC-ODO and in BNL, USA
Effort going on in Daresbury (Cockcroft Institute and STCF) with CERN.

## Slide 38: Progress in SC Crab Cavities
Finished cavity at Niowave
Jan 2012
May 2012
UK - Cockcroft
USA (ODU)

## Slide 39: Crab cavity ; cryomodule and cavity
Y. Yakovlev et al.
~250 mm outer radius
L. Xiao et al.

## Slide 40
IP1
Q3,Q2,Q1
DFBX
D1
Q4,D2
Q5
Q6
DFBL
DFBA
Q11, Q10…Q7
IP 8
TAS
TAN
4.5 K
4.5 K
1.9 K
12 m
3 m
3.6 m
UJ 13
RR 13
SC Links
Layout at Point 1
A. Ballarino, 18 Nov. 2011
I
I

## Slide 41
DFB in the tunnel at P1 L
A. Ballarino, 18 Nov. 2011

## Slide 42
Room temperature
Cryogenic environment
(4.5 K LHe in the DFBs)
Tunnel
Cold powering system:
1) Current leads in a distribution cryostat (near the power converters);
2) Vertical electrical transfer (link);
3)Horizontal electrical transfer (link);
4) Cryogenic fluid supply and control;
5) Interconnection to the magnets bus system;
6) Protection of link and current leads.

## Slide 43
2100 kA
A. Ballarino, 18 Nov. 2011

## Slide 44
MgB2 Tape : 3.640.65 mm2
MgB2 : 12 %
Cu : 15 %
MgB2
YBCO
YBCO Tape : 4 0.1 mm2
YBCO: 1-3 m
Cu : 220 m
Bi-2223
Bi-2223 Tape : 4.5 0.4 mm2
BSCCO: 23 %
Cu : 250 m
A. Ballarino, 18 Nov. 2011
Conductors in Superconducting Links

## Slide 45
A. Ballarino, 18 Nov. 2011
Nb-Ti cables
used in LHC
6 kA at 6 K
MgB2 cable
6 kA at 20 K
(> 12 kA at 4.5 K)
6 mm
Minimum quench energy of superconductors
Nb-Ti, Top = 5 K
Tc= 6 K → MQE = 2.63 mJ/cm3
Tc = 7 K → MQE = 5.26 mJ/cm3
Tc = critical temperature
Top = operating temperature
MQE= Minimum Quench Energy

## Slide 46: PLAN First installation SC link 2017?
Horizontal SC link in P7: RR with many 600 A EPCs in RR just downstream betatron cleaning
Nexan Cryoflex® line (20 m long cryostat of link) procured and
installed in the CERN SM-18 laboratory
20 kA – 4 to 80 K test

## Slide 47: Beam Diagnostic & Instrumentation
BPM capable to withstand more intense beam
Cryo BLM
Long range beam wire for LRBB compensation
Experiments in SPS and RHIC demonstrated ability to affect the beam (destroy it) but not yet to cure it (we can only do i LHC)
It is a collimator like device: 10  or less form beam

## Slide 48: E-lens? From FNAL?

## Slide 49: LS2 - 2018
Cryogenics P4  separation between SC Magnets and RF Cavities cooling circuit
5-6 kW plant
crab cavity test P4
Anticipated 2017:
  Sc link in P7
  Test crab cavities in SPS

## Slide 50: LS2 - 2018
DS Cryo-collimation with 11 T in 1 IP: priority NOT yet decided: IP1,IP5 or IP2 ? Review of collimation needs in Spring 2013
Vertical SC links in RRs of P1, P5 (stand-alone)
Improve triplet cooling
Some Beam diagnostics
Some Collimators
INJECTORS!

## Slide 51: LS3
Triplets + D1-D2 (disinstallation)
TAS + Exp-interfaces
New cryo in IP1-IP5 with separation Arc-IR
New MS magnets (Q4-Q5) and correctors
CC cavities with its local cryo
Vertical links for all new magnets IP1-IP5
New collimators
Diagnostics & wigglers

## Slide 52: FP7 HiLumi Design Study application 25 Nov 2010

## Slide 53: HiLumi is the focal point of 20 years of converging International collaboration
The collaboration wiht US on LHC upgrade started during the construction of LHC
EU programs have been instrumental in federating all EU efforts
With Hi-Lumi the coordination makes a step further: from coordinated R&D to a common project
CERN is not anymore the unique owner, rather is the motor and cathalizer of a wider effort.
Managed like a large detector collaboration (with CERN in special position as operator of LHC)

## Slide 54: Budget FP7 HiLumi
Waiving effect
CERN waives all technical works: LHC is core program.
Only kept the CERN cost for managem.
50%
85% of CERN gen. mngt
Only EU research area
Perfect score 15/15, 100% budget

## Slide 55: HL-LHC management

## Slide 56: HL-LHC composition
Collimation
Project
Matching section and correctors
Beam Diagnostics
High Field Magnets R&D
HE-LHC Studies
Hardware Commissioning
5 M€ grant from EC FP7

## Slide 57: Budget of HiLumi DS and HL-LHC
HiLumi covers 6 WPs
Manag and Tech. Coord. (6%)
Acc. Physics and beam
Magnets for IR
Crab Cavities
Collimators
Sc links
 | Improving Consolidation | Full performance | Total HL-LHC
Mat. (MCHF) | 476 | 360 | 836
Pers. (MCHF) | 182 | 31 | 213
Pers. (FTE-y) | 910 | 160 | 1070
TOT (MCHF) | 658 | 391 | 1,049
Table 2. Summary of the cost of HL-LHC with split between Performance Improving-Consolidation and Full performance i.e. all HL-LHC)

## Slide 58: Lumi reach in the two cases

## Slide 59: And after? Can we run LHC forever?
NO: history demonstrates that at certain point, to get resources for new projects, previous accelerators are closed (despite last minute claims of new discovery…)
High Energy LHC may be the answer

## Slide 61: Possible list of parameters

## Slide 62: List parameters - cont.

## Slide 63: Main dipoles: is it possible ?
Looking at performance offered by practical SC, considering tunnel size and basic engineering (forces, stresses, energy) the practical limits is around 20 T. Such a challenge is similar to a 40 T solenoid (-C)
Nb-Ti operating dipoles;
Nb3Sn block test dipoles
Nb3Sn cos test dipoles

## Slide 64: The Superconductor « space »
Chart: Applied Field (T)
| 0 | 5 | 15 | 20 | 25 | 30
YBCO: Parallel to tape plane, 4.2 K | 4144.6766 | 3507.9375 | 3148.3332 | 2909.0554 | 2090.4933 | 1888.9952
YBCO: Perpendicular to tape plane, 4.2 K | 4144.6766 | 1445.8386 | 975.0997 | 767.7508 | 655.6687 | 571.6114 | 526.7777 | 481.944 | 442.7183 | 428.1462 | 403.4904 | 386.6773 | 364.2626 | 341.8457 | 328.3952 | 319.4289 | 318.3073
2212: Round wire, 4.2 K | 1265.6716 | 1257.7114 | 1257.7114 | 1225.8706 | 1181.0945 | 1126.3682 | 1040.796 | 973.1343 | 929.3532 | 835.8209 | 780.0995 | 704.4776 | 623.8806 | 577.7114 | 529.3532 | 513.4328 | 509.4527 | 489.5522 | 469.6517 | 453.7313 | 435.8209 | 416.9154 | 398.01 | 380.0995 | 364.1791 | 347.2637 | 330.3483 | 315.4229 | 298.5075 | 282.5871 | 265.4726
Nb3Sn: High Energy Physics, 4.2 K | 1754.8557 | 1454.9349 | 1190.9814 | 1072.6374 | 957.7741 | 855.0933 | 757.6336 | 268.0143 | 190.8587 | 118.9241 | 65.5533 | 28.3097
Nb-Ti (LHC) 1.9 K | 1430 | 1195.7692 | 950.7692 | 703.4615 | 475.7692
Nb-Ti
Nb3Sn
HTS

## Slide 65: The « new » materials: HTS Bi-2212
DOE program 2009-11 in USA let to a factor 2 gain. We need another 50% and more uniformity, eliminating porosity and leakage
Round wire, isotropous and suitable to cabling!
HEP only users (good < 20K and for compact cable)
Big issue: very low strain resistance, brittle
Production ~ 0,
cost ~ 2-5 times Nb3Sn (Ag stabilized)

## Slide 66: The « new » materials: HTS YBCO
Tape of 0.1-0.2 mm x 4-10 mm : difficult for compact (>85%) cables
Current is EXCELENT but serious issue is the anisotropy;
>90% of world effort on HTS are on YBCO! Great synergy with all community
Cost : today is 10 times Nb3Sn, target is same price: components not expensive, process difficult to be industrialize at low cost
FP7 Eucard is developing EU Ybco

## Slide 67: New (old) approach to cabling suitable for tapes
An old type of cabling (Roebel) suitable for tapes has been recently rivisited (Karlsruhe, New Research Industry NZ)
Here a first 2 m long test cable done at CERN

## Slide 68: Magnet shapes (field optimization & structure)
Cos Coil
Block Coil
Canted Solenoid Coil
Hybrid Cos Block Coil
P. McIntyre
S. Caspi

## Slide 69: First consistent cross section, 2010 WG and Malta (fits our tunnel)
Magnet design: 40 mm bore (depends on injection energy: > 1 Tev) Very challenging but feasable: 300 mm inter-beam; anticoils to reduce flux
Approximately 2.5 times more SC than LHC: 3000 tonnes!
Multiple powering in the same magnet for FQ (and more sectioning for energy)
Certainly only a first attempt: cos and other shapes will be also investigated
L. Rossi and E. Todesco

## Slide 70: The EU program The chance for HTS
Last FP7 call in Nov2011: EuCARD2 (2013-16)
Approved; under negotiation for signature
WP-10Future Magnets
  Assessment of YBCO and Bi-2212 for HE-LHC
  Development of 10 kA class HTS compact cable
  Prototype of a 5 T real accelerator quality magnet
  Test the coil in a 13-15 T background field to proof 18-20 T principle with 10 kA HTS conductor.

## Slide 71: What is the possibile for HE-LHC?
2005 2010 2015 2020 2025 2030 2035
US 16 T small dipole
EuCARD 13 T large dipole+ 18 T small insert
US 13 T Quads FP7-HiLumi
US NbSn-HTS development
15-20 T dip final proto & Industrialization
Final delivery Magnets HE-LHC
HE-LHC start-up
HE-LHC preliminary study
HTS for HE-LHC: yes.or.no
LARP 11 T long quad
EuCARD R&D
Industry contracts, start constrution
US basic programs and LARP R&D
EU FP6-CARE-NED
EuCARD2 full bore dipole HTS
15-20 T R&D dipole models and prototypes
Full profit of the HiLumi program

## Slide 72: Other important issues (among many …)
Synchrotron radiation
15 to 30 times!
The best is to use a window given by vacuum stability at around 50-60 K (gain a factor 15 in cryopower removal!)
First study on beam impedance seems positive but to be verified carefully
Use of HTS coating on beam screen?
Beam in & out
Both injection and beam dump region are constraints.
Ideally one would need twice stronger kickers
Beam dumps seems feasable by increasing rise time from 3 to 5s
Injection would strongly benefit form stronger kickers otherwise a new lay-out is needed (different with or wihtout experiments)

## Slide 73: Injector chain
Various reason to renew
Age! PS 80 years old by 2039
SPS will have seen an amount of radiation well beyond its design
Chance to redesign the chain in synergy with other programs
  Low energy physics
  Neutrino
SPS+ (1-1.2 TeV) R&D is progressing thanks to FAIR SIS300 design.
Discorap INFN magnet, 4.5 T pulsed at 1-2 T/s, test in July : success

## Slide 74: Between Linac4 and SPS+
HE-LHC
Linac4
SPS+
New injectors optimization

## Slide 75: Alternate scenarios for Injectors
Avoid touching the SPS (and its transfer lines: 6 km!)
Install a Low Energy Ring in the LHC tunnel using superferric Pipetron magnets (W. Foster). Possible with adequate logistic and change in the experiment (workshop 2006 FP6-CARE-HHH network, revisited for LHeC ring-ring option).
Work done in collaboration with Fermilab (H. Piekartz)

## Slide 76: The big leap forward: a 80 km tunnel for a VLHC
For a LEP300?, then for HE-LHC
Optimitation could be at 16 T field level: collision energy 80 TeV c.o.m.
Much better new infrastructure.
However many costs go linearly, or more, with length. Magnet stored energy, beam energy also a concern
Whatever solution, a vigorous Magnet R&D will enable to go beyond LHC energy
Option 1 (preferred)
Option 2
John Osborne (CERN), Caroline Waaijer (CERN)