## Slide 1: Marui Galvanizing Co ., Ltd. Corporate History
Established in 1957
55 Years of Metal Surface Process Experiences
Location
HQ = Hyogo, Japan
Himeji Factory = Hyogo, Japan
Kashiwa Factory = Chiba, Japan
Tohoku Factory = Aomori, Japan
Subsidiary
South Korea
China
Himeji Castle

## Slide 2: Factory & Facility
Kashiwa Factory
Inside the Factory
RO Facility
Reuse
Recycle
Reduce
Recycled Metal

## Slide 3: Varieties of Electro-polishing
Vacuum EQPT
Medical Use
Chamber for display
Chemical Tank
Heat Exchanger

## Slide 4: We are heading for
Highest Electro-polishing Technology on
Metal Surface: SUS, Al, Ti, FeO, Nb & etc.
Participate as an EP Supplier into the Linear Accelerating World
Vertical EP Mass-Production in the most efficient & appropriate way

## Slide 5: New Method of Vertical Electro-Polishing on ILC Cavity
As a Result of Joint Research with KEK.
Marui Galvanizing Co.,Ltd.

## Slide 6: Introduction
Thanks to the joint research with KEK on ILC, we have been studying vertical electro-polishing on ILC cavity since June 2012.
We, Marui Galvanizing Co. Ltd, are under development of very unique new vertical electro-polishing method herein in cooperation with KEK/ILC group.

## Slide 7: Contents
1. Outstanding issues (by using SUS model)
Removal of hydrogen gas generated while EP.
2. Approach & effort
Development of i-cathode “Ninja” TM
Features of the i-cathode “Ninja” TM
Features of integrated new VEP system.
3. Next step plan 1 & 2

## Slide 8: 1. Outstanding Issues
According to our past several experiments by using SUS Cavity, lower part of cavity was well electro-polished, however, upper part of cavity was not well polished.
We suppose this because the electric current did not flow evenly due to the hydrogen gas generated during EP process.

## Slide 9
Features of i-cathode “Ninja” TM Already applied International Patent
Rotatable Variable Wings
Unfold i-cathode
“Ninja” TM and
rotate while EP
Insert i-cathode
“Ninja” TM
2. Approach & Effort

## Slide 10
To remove hydrogen gas generated during EP process by the method of fluid circulation.
A part of features : Integrated New VEP System
EP electrolyte circulation
Flow direction
Acid bath
Pump

## Slide 11: 3. Next Step Plan 1 – EP on Nb. Cavity
Trial vertical EP on Nb single-cell cavity by MG – the end of April 2013
Flanges needs to be set up by KEK on this cavity.
We hope this to be evaluated by KEK / CEA Saclay.
Furthermore, we would like to challenge EP of Nb 9-cell cavity around July 2013 in vertical manner. Currently looking for available Nb 9-cell cavity for next trial VEP.
MG purchased from RI GmbH
Inside the Nb.One Cell Cavity

## Slide 12: 3. Next Step Plan 2 – Development of total system
1. Manufacturing In Process Pre-EP (MIPPEP) TM
Each dumbbell prior to welding to be pre-electro-polished
for the purpose of minimizing material defects.
2. Development of pure steam cleaning.
3. Development of total package on vertical electro-polishing by adopting computerized control system.
4. Development of wastewater disposal system.