## Slide 1: Summary of STF-EP facility at KEK.
Motoaki.Sawabe
Radiation Science Center, Applied Research Laboratory, KEK

## Slide 2
STF
1. Location of STF-EP facility at KEK.
STF building.

## Slide 3
Equipment | Amount | Note
EP bed | 2 | No.1 , No.2
EP-electrolyte reservoir tank | 2 | No.1 (2000L) , No.2 (500L)
Heat exchange | 2 | No.1 , No.2
Current rectifier | 2 | No.1 , No.2 50V,1000A
Ultra sonic washing bath | 2 | No.1 , No.2 2m3 , 36kHz, 600W×8
Ultra pure water unit | 2 | No.1 , No.2
High pressure rinse unit (HPR) | 1 | 8MPa , Ultra pure water
Absorption tower | 1 | Two tower type , For exhaust gas.
Waste water tank | 2 | 10m3×2
EP equipment for examination | 1 | We call “ Lab.EP” , 30V,50A
2. List of main equipments.

## Slide 4
No.1 EP bed
No.2 EP bed
No.1 Reservoir tank (2000L)
No.2 Reservoir tank (500L)
No.2 Ultrasonic washing bath
No.1 Ultrasonic washing bath
HPR
Heat exchange
Control room
3.Equipments installation.
No.1 EP area
Height 2.5M

## Slide 5
STF-EP facility area.
No.1 EP area.
The area is cleaned by four air filters.
No.1 EP hut.
No.1 EP bed and 9cell cavity.
No.2 EP hut.
No.2 EP bed and 500MHz Single cell cavity.
4. Picture of main equipments. (1)
Cooling air duct
Cooling air cover
Cooling air fan
Air filter

## Slide 6
No.1 Reservoir tank .( Max.2000L )
No.2 Reservoir tank .( Max. 500L )
No.1 Current rectifier.
Max. 50V, 1000A
No.1 Ultrasonic washing bath and 9cell cavity.
No.1 Ultrasonic oscillators
36kHz , 600W ×8.
Robot arm. (for cavity movement. )
In No.1 EP area.
4. Picture of main equipments. (2)

## Slide 7
High pressure rinse unit. ( HPR )
HPR and 9cell cavity.
No.2 Ultra pure water unit.
About 25L/min. (Ultra pure water)
Absorption tower. ( for exhaust gas.)
Alkaline water washing. (pH 10 )
Waste water tanks. (10m3×2 )
We call “ Lab.EP “.
4. Picture of main equipments. (3)

## Slide 8
100μm,Electric current density 50mA/cm2, at No.2 EP-bed or No.1
1st coarse pure water washing 60min.
Ultrasonic washing by detergent ( 2% FM-20) at 50℃,15min.
High pressure rinsing 1Hr.
1) In the case of EP1 ( Bulk EP )
5. Flow of the EP processing.
After open the cavity ,pure water rinsing.
After open the cavity ,pure water rinsing.

## Slide 9
5～20μm,Electric current density 35～40mA/cm2, at No.1 EP-bed,
Cavity surface temperature <35℃
1st coarse pure water washing 90min.(Filled with water, and vibration.)
Ultrasonic washing by detergent ( 2% FM-20 ) at 50℃,15min.
High pressure rinsing 8Hr.
Detergent brush washing by hand in beam pipes.
2) In the case of EP2 ( Finish EP )
After open the cavity ,pure water rinsing.
After open the cavity ,pure water rinsing.
After open the cavity ,pure water rinsing.

## Slide 10
Thermocouples and transmitter for cavity surface temperature. ( 12ch. )
Air cooling ducts and cover.
Vibrator.
Vibration at pure water washing.
Brush washing by hand in beam pipes and antennas.
Exclusive brushes.
Vibrator.
Vibrator.

## Slide 11
The electro-polishing (EP) facilities in KEK were completed at STF (Super conducting RF Test Facility) area in Dec, 2007. And we have begun to operate in Feb, 2008.
In this facility, the capacity of the electrolyte reservoir tank is 2,000 L (Figure 1). It is very large. We put the EP-electrolyte of 2,000kg (≒ 1,100L) into this tank. And we use it repeatedly many times.
The laboratory doing such a usage is only here.
We changed the EP-electrolyte four times until
now.
And we are using the 5th-period EP-electrolyte.
No.1 reservoir tank ( 2,000L )
6. History of STF-EP facility at KEK.

## Slide 12
EP-electrolyte | The period of EP | The number of times of EP-processing （Except Pre EP） | Total theoretical removal weight（g） | Final niobium concentration（g/L）
1st period EP-electrolyte | Feb, 2008 ～ May 2009 | 41 | 9,433 | 8.6
2nd period EP-electrolyte | May 2009 ～ July 2010 | 59 | 10,174 | 9.8
3rd period EP-electrolyte | July 2010 ～ July 2011 | 43 | 13,032 | 12
4th period EP-electrolyte | July 2011 ～ May 2012 | 38 | 11,708 | 12
5th period EP-electrolyte | May 2012 ～ |  |  | 
Lower list shows the history of EP-electrolyte that had been used until now.

## Slide 13
Date | Cavity | Performance (MV/m) | Notice
July.28,2010 | ERL2cell#2 | 38.4 | 
Oct.20,2010 | MHI9cell#A | 29.1 | Non HOM
Nov.04,2010 | MHI9cell#12 | 37.7 | 
Nov.17,2010 | MHI9cell#13 | 36.4 | Achievement of ILC spec.
Dec.01,2010 | MHI9cell#12 | 40.7 | Achievement of ILC spec.
Dec.15,2010 | MHI9cell#13 | 33.1 | 
May.25,2011 | MHI9cell#17 | 39.2 | Achievement of ILC spec.
Jun.08,2011 | MHI9cell#14 | 36.6 | Achievement of ILC spec. at niobium concentration about 10g/L
Jun.22,2011 | ERL2cell#3 | 30.3 | 
Lower list shows the cavity performance results by the 3rd-period EP-electrolyte.
In this electrolyte, we could achieve ILC spec in the four cavities.
We could achieve it by the EP-electrolyte aged enough.
Niobium concentration at this time was about 10 g/L.
And in the 4th EP-electrolyte, we could achieve it at 11g/L.
In thinking about the life (exchange time) of EP-electrolyte, it will be the big result.
7. The cavity performance result by the aging.
Fine.