## Slide 1
Magnetic Micro-Calorimeters
for Astro-Particle Physics
Loredana Gastaldo Kirchhoff-Institute for Physics, Heidelberg University

## Slide 2
Low temperature micro-calorimeters
G
t
T
E
Ctot
Thermal bath
E = 10 keV
 1 mK
Ctot = 1 pJ/K
Very small volume
Working temperature below 100 mK
small specific heat
small thermal noise
Very sensitive temperature sensor

## Slide 3
Temperature sensors
Resistance of highly doped semiconductors
R
T
R
T
Resistance at superconducting transition,TES
Magnetization of paramagnetic material
M
T

## Slide 4
Paramagnetic sensor: Au:Er500ppm
Signal size:
M
T
Metallic Magnetic Calorimeters - MMC
main differences to calorimeters with resistive thermometers
no dissipation in the sensor
no galvanic contact to the sensor

## Slide 5
MMC: signal size
Au:Er 300 ppm
Inverse Temperature T1 [K 1]
Magnetization M [A/m]
Au:Er 300 ppm
Temperature T [mK]
Specific heat C [104 J mol1K1]
Au:Er 300 ppm
Numerical calculations based on mean field approximation are used to describe thermodynamical properties of interacting spins (RKKY)

## Slide 6
Two-stage SQUID setup with flux locked loop allows for:
low noise
large bandwidth / slewrate
small power dissipation on detector SQUID chip (voltage bias)
T ~ 30 mK
T ~ 300 mK
MMCs: Readout

## Slide 7
Well established:
planar T-sensor
superconducting meander shaped pickup loop
B-field generated by persistent current
transformer coupled to SQUID
New sandwich geometry:
best magn. flux coupling,
planar sensor
sandwiched between stripline
MMCs: Geometries

## Slide 8
Mask writer
Wet bench
Chemistry
Dry etching
Mask aligner
UHV sputtering
Cleanroom facilities at KIP
MMCs: Microfabrication
Flexibility in design and fabrication
Reliable processes for thin films
Presently 10 different designs (6-16 layers) processed in parallel

## Slide 9
Typical non-linearity:
1-3% at 6 keV
maXs20: 1d-array for soft x-rays
1×8 x-ray absorbers
  250mm×250mm gold, 5mm thick
  98% Qu.-Eff. @ 6 keV
  electroplated into photoresist mold (RRR>15)
  mech/therm contact to sensor by stems to prevent loss of initially hot phonons
Au:166Er300ppm temperature sensors
  co-sputtered from pure Au and high conc. AuEr target
Meander shaped pickup coils
  2.5 mm wide Nb lines
  Ic ≈ 100mA
On-chip persistent current switch (AuPd)
250 mm
Au:Er
on
Nb meander

## Slide 10
Typical non-linearity:
1-3% at 6 keV
maXs20: 1d-array for soft x-rays
Fastest rise-time among
µ-cal for x-ray detection
rise time: 90 ns @ 30 mK,
as expected for the spin-electron-relaxation
from Korringa-constant of Er in Au

## Slide 11
Typical non-linearity:
1-3% at 6 keV
maXs20: 1d-array for soft x-rays
decay time here: 3 ms @ 30 mK
nearly single exponential decay
On-chip thermal bath
magnetic flux
time
adjusted by sputtered
thermal link (Au)
G

## Slide 12
 1 %
DE [eV]
Typical non-linearity:
1-3% at 6 keV
maXs20: 1d-array for soft x-rays
Photon energy E [keV]
Measured energy E [keV]
Relative signal amplitude A
non-linearity: 1% at 6 keV
as expected from thermodynamical properties
well described by quadratic term
The energy scale is defined
with high precision

## Slide 13
241Am
maXs20: 1d-array for soft x-rays
non-linearity: 6% at 60 keV
as expected from thermodynamical properties
well described by quadratic term

## Slide 14
Typical non-linearity:
1-3% at 6 keV
maXs20: 1d-array for soft x-rays (T=20 mK)
Very good energy resolution
DEFWHM= 1.6 eV @ 6 keV

## Slide 15
DEFWHM = 1.5 eV @ 0 keV
Live !
maXs20: 1d-array for soft x-rays (T=20 mK)

## Slide 16
maXs20: 1d-array for soft x-rays (T=20 mK)
Large dynamic range

## Slide 17
maXs200: 1d-array for hard x-rays
1x8 x-ray absorbers
2 mm x 0.5 mm
200 mm thick electroplated Au
80% QE at 100 keV
DEFWHM < 50 eV
photo resist mold
electroplated Au absorbers

## Slide 18
side arm without radiation shields
maXs-200
Amplifier SQUIDs
16 pixels maXs-200 on detector platform
maXs200 on cold finger of a dry cryostat

## Slide 19
maXs200 – 241Am calibration source
DEFWHM = 60 eV @ 60 keV
DEFWHM = 40 eV @ 0-20 keV
237Np
Slight degradation towards higher energies due to position dependence, Meanwhile fixed by stems between absorber and sensor
237Np
237Np

## Slide 20
Large Arrays – parallel read-out
maXs-20/30/200:
8×8 pixels for photons up to 20/30/200 keV
with DEFWHM = 2/5/30 eV
32 two-stage dc-SQUIDs
2, 4, 8 mm

## Slide 21
Large Arrays – parallel read-out
How could one increase the number of pixels?

## Slide 22
Pixel identification
via rise-time
of the detector signal
heat bath
absorber
thermal link
sensor
stems
Porst et al., AIP Conf. Proc. 1185 (2009) 599
The Hydra principle

## Slide 23
Read out scheme

## Slide 24
Read out scheme

## Slide 25
Read out scheme

## Slide 26
+
-
Read out scheme
+
-

## Slide 27
Read out scheme
+
-
+
-

## Slide 28
4.5 cm
~
64 × 64 pixels
200 eV (FWHM)
32 × 32 temperature sensors
Read out by 16 + 16 SQUIDs
MOCCA: a 4k-pixel MMC camera

## Slide 29
But:
  number of wires
  parasitic heat load
  costs
  complexity
multiplexing scheme required
(TDM, FDM, CDM, …)
Simplest idea: duplicate single channel readout
N
Brute force read-out of 8x8 x-ray detectors
How to read-out 1000s of high-res detectors?

## Slide 30
IN
OUT
Microwave SQUID Multiplexer for the Readout of Metallic Magnetic Calorimeters S.Kempf et al., J. Low. Temp. Phys. 175 (2014) 850-860
Single HEMT amplifier and 2 coaxes to read out 100 - 1000 detectors
No events
Event in 3
MMCs: Microwave SQUID multiplexing

## Slide 31
9.1 mm
15.5 mm
Elbow coupler
MMC
rf-SQUID
MMCs: Microwave SQUID multiplexing

## Slide 32
Successful production and
test of the first prototype
MMCs: Microwave SQUID multiplexing
M. Wegner et al., in preparation

## Slide 33
Neutrino mass determination

1 meV
10 meV
1 eV

## Slide 34
The Electron Capture in 163Ho experiment
Department of Nuclear Physics, Comenius University, Bratislava, Slovakia
Fedor Simkovic
Department of Physics, Indian Institute of Technology Roorkee, India
Moumita Maiti
Goethe Universität Frankfurt am Main
Udo Kebschull, Panagiotis Neroutsos
Institute for Nuclear Chemistry, Johannes Gutenberg University Mainz
Christoph E. Düllmann, Klaus Eberhardt, Holger Dorrer, Fabian Schneider
Institute of Nuclear Research of the Hungarian Academy of Sciences
Zoltán Szúcs
Institute of Nuclear and Particle Physics, TU Dresden, Germany
Kai Zuber
Institute for Physics, Humboldt-Universität zu Berlin
Alejandro Saenz
Institute for Physics, Johannes Gutenberg-Universität
Klaus Wendt, Sven Junck, Tom Kieck
Institute for Theoretical and Experimental Physics Moscow, Russia
Mikhail Krivoruchenko
Institute for Theoretical Physics, University of Tübingen, Germany
Amand Fäßler
Institut Laue-Langevin, Grenoble, France
Ulli Köster
Kirchhoff-Institute for Physics, Heidelberg University, Germany
Christian Enss, Loredana Gastaldo, Andreas Fleischmann,
Clemens Hassel, Sebastian Kempf, Mathias Wegner
Max-Planck Institute for Nuclear Physics Heidelberg, Germany
Klaus Blaum, Andreas Dörr, Sergey Eliseev, Mikhail Goncharov,
Yuri N. Novikov, Alexander Rischka, Rima Schüssler
Petersburg Nuclear Physics Institute, Russia
Yuri Novikov, Pavel Filianin
Physics Institute, University of Tübingen, Germany
Josef Jochum, Stephan Scholl
Saha Institute of Nuclear Physics, Kolkata, India
Susanta Lahiri
The Electron Capture 163Ho Experiment: ECHo
L. Gastaldo et al., JLTP 176 - 5 (2014) 876-884

## Slide 35
163Ho and neutrino mass
n
p
p
p
n
n
e-
e-
e-
e-
n
p
p
p
n
n
n
e-
e-
p
e-
e-
e-
Atomic de-excitation:
X-ray emission
Auger electrons
Coster-Kronig transitions
A non- zero neutrino mass affects the de-excitation energy spectrum
Calorimetric
measurement
Source
.
.
.
.
.
.
.
1/2  4570 years
QEC = (2.555  0.016) keV
(2*1011 atoms for 1 Bq)
M. Wang, G. Audi et al., Chinese Phys. C 36, 1603, (2012)

## Slide 36
163Ho QEC-value
1/2  4570 years
QEC = (2.555  0.016) keV
(2*1011 atoms for 1 Bq)
M. Wang, G. Audi et al., Chinese Phys. C 36, 1603, (2012)
Calorimetric measurements
Measurements of x-rays
Gatti et al., 1997
ECHo, 2012

## Slide 37
1/2  4570 years
QEC = (2.555  0.016) keV
(2*1011 atoms for 1 Bq)
Penning Trap Mass Spectroscopy
“Direct measurement of the mass difference of 163Ho and 163Dy
as prerequisite to a determination of the electron neutrino mass”
S. Eliseev et al., Phys. Rev. Lett., 115, 062501 (2015)
QEC = (2.833  0.030stat  0.015syst) keV
M. Wang, G. Audi et al., Chinese Phys. C 36, 1603, (2012)
163Ho QEC-value
Calorimetric measurements
Measurements of x-rays
Gatti et al., 1997
ECHo, 2012
Independent of 163Ho decay parameters

## Slide 38
1/2  4570 years
QEC = (2.555  0.016) keV
(2*1011 atoms for 1 Bq)
Penning Trap Mass Spectroscopy
QEC = (2.833  0.030stat  0.015syst) keV
M. Wang, G. Audi et al., Chinese Phys. C 36, 1603, (2012)
163Ho QEC-value
Calorimetric measurements
Measurements of x-rays
Gatti et al., 1997
ECHo, 2012
Independent of 163Ho decay parameters
To reduce uncertainties in the analysis:
QEC determination within 1 eV
 PENTATRAP (MPIK HD)
“Direct measurement of the mass difference of 163Ho and 163Dy
as prerequisite to a determination of the electron neutrino mass”
S. Eliseev et al., Phys. Rev. Lett., 115, 062501 (2015)

## Slide 39
MI
MII
NI
NII
OI
OII
OI
163Ho and neutrino mass

## Slide 40
Statistics in the end point region
Nev > 1014 → A ≈ 1 MBq
Unresolved pile-up (fpu ~ a  r)
fpu < 10-5
r < 1 µs  a ~ 10 Bq
105 pixels
Precision characterization of the endpoint region
EFWHM < 3 eV
Low temperature
Metallic Magnetic Calorimeter
fpu = 10-5 EFWHM = 3 eV
Requirements for sub-eV sensitivity in ECHo

## Slide 41
Meander
Source
Sensor
Absorber for calorimetric measurement
 ion implantation @ ISOLDE-CERN
About 0.01 Bq per pixel
Operated over more then 4 years
First detector prototype
L. Gastaldo et al.,
Nucl. Inst. Meth. A, 711 (2013) 150
P. C.-O. Ranitzsch et al.,
http://arxiv.org/abs/1409.0071v1
Absorber

## Slide 42
Rise Time ~ 130 ns
EFWHM = 7.6 eV @ 6 keV (2013)
EFWHM = 2.4 eV @ 0 keV (2014)
Non-Linearity < 1% @ 6keV
Synchronized measurement of 2 pixels
Presently most precise 163Ho spectrum
MII
MI
NII
NI
144Pm
OI
First calorimetric measurement of the OI-line
 | EH bind. | EH exp. | H lit. | H exp
MI | 2.047 | 2.040 | 13.2 | 13.7
MII | 1.845 | 1.836 | 6.0 | 7.2
NI | 0.420 | 0.411 | 5.4 | 5.3
NII | 0.340 | 0.333 | 5.3 | 8.0
OI | 0.050 | 0.048 | 5.0 | 4.3
P. C.-O. Ranitzsch et al ., http://arxiv.org/abs/1409.0071v1)
L. Gastaldo et al., Nucl. Inst. Meth. A, 711, 150-159 (2013)
QEC = (2.843  0.009stat - 0.06syst) keV
Calorimetric spectrum

## Slide 43
MII
MI
NII
NI
144Pm
OI
Detector design and fabrication:
Increase activity per pixel
Remove low energy tail
Understanding of the 163Ho spectrum:
Investigate undefined structures
High purity 163Ho source:
Background reduction
144Pm
Where to improve
NI

## Slide 44
Requirement : >106 Bq  >1017 atoms
(n,)-reaction on 162Er
- High cross-section
- Radioactive contaminants  need of chemical separation
Summer 2013: Two irradiations at ILL
- Treatment of Er prior to irradiation:
- Treatment of Er after irradiation:
- 30 mg for 55 days  1.6•1018 atoms 163Ho
- 7 mg for 7 days  1.4•1016 atoms 163Ho
Source production and separation
: (n,)-reaction on 162Er
High purity 163Ho source
Thermal neutron flux (): 1.3x1015 cm-2s-1

## Slide 45
Requirement : >106 Bq  >1017 atoms
(n,)-reaction on 162Er
- High cross-section
- Radioactive contaminants
Excellent chemical separation
Available 163Ho source:
~ 1018 atoms
Source production and separation
Only 166mHo
: (n,)-reaction on 162Er
High purity 163Ho source
ECHo requirements:
166mHo/ 163Ho < 10-9
Offline mass separation:
RISIKO, Mainz University
ISOLDE-CERN

## Slide 46
Separation at CERN/ISOLDE December 2014
Chemically purified 163Ho source
Offline implantation @ISOLDE-CERN using GPS and RILIS
High purity 163Ho source: Mass separation
- RISIKO mass-separator @ Uni-Mainz: successful tests with natural Ho:
Optimized resonant laser ionization for Ho
Focalization of the beam for implantation onto sub-mm detector absorber

## Slide 47
New detectors: first results
MI
MII
NI
NII
OI
OLD (more then 1 month )
NI
OI
MI
NII
MII
preliminary
Activity per pixel A ~ 0.2 Bq
Baseline resolution EFWHM ~ 5 eV
Symmetric detector response
No strong evidence of radioactive contamination in the source
NEW ( about 2 days)

## Slide 48
Background
Background sources:
Environmental radioactivity Material screening
Cosmic rays Underground labs
Induced secondary radiation by cosmic rays μ-Veto
Radioactivity in the detector
Study of background sources through:
Monte Carlo simulations
Dedicated experiments
Underground
measurements in Modane
on going
Background level
510-5 counts/eV/det/day
Screening facilities
Uni-Tübingen
Felsenkeller

## Slide 49
Prove scalability with medium large experiment ECHo-1K
  A  1000 Bq High purity 163Ho source (produced at reactor)
  EFWHM < 5 eV
  r< 1 µs
  multiplexed arrays  microwave SQUID multiplexing
  1 year measuring time 1010 counts = Neutrino mass sensitivity m < 10 eV
ECHo-1M towards sub-eV sensitivity
ECHo outlook
Research Unit FOR 2202/1
„Neutrino Mass Determination by Electron Capture in Holmium-163 – ECHo“

## Slide 50
Search for neutrinoless double beta decay
?

## Slide 51
Neutrinoless double beta decay
2: (A,Z) → (A, Z+2) + 2e- + 2e
1/2 ≈ 1020 years
If  =  :
0: (A,Z) → (A, Z+2) + 2e-
1/2 > 1025 years
Measured for several nuclides
Never observed
If conservation rules don´t allow simple beta decay:

## Slide 52
Neutrinoless double beta decay
2: (A,Z) → (A, Z+2) + 2e- + 2e
1/2 ≈ 1020 years
If  =  :
0: (A,Z) → (A, Z+2) + 2e-
1/2 > 1025 years
Measured for several nuclides
Never observed
If conservation rules don´t allow simple beta decay:
Identification and reduction of background sources

## Slide 53
photon sensor
phonon sensor
Scintillating crystals
The energy of an interacting particle
is converted into heat and light
The fraction of light depends on the mass of the particle
Measure both fractions of energy
 discrimination
 rejection of background events
D.V. Poda et al., LUMINEU EDELWEISS Collaboration
arXiv:1502.01161 [physics.ins-det]

## Slide 54
photon sensor
phonon sensor
Scintillating crystals
The energy of an interacting particle
is converted into heat and light
The fraction of light depends on the mass of the particle
Measure both fractions of energy
 discrimination
 rejection of background events
Low T thermal detectors are the best
candidate for these measurements

## Slide 55
AMoRe and LUMINEU
Investigation of with scintillating crystals
AMoRE
Advanced Mo-based Rare process
Experiment
CaMoO4 scintillating crystals
MMC for photon and phonon channel
LUMINEU
Luminescent Underground Molybdenum Investigation for NEUtrino mass and nature
ZnMoO4 scintillating crystals
NTD-Ge baseline for photon and phonon channel
MMC R&D for photon channel

## Slide 56
AuEr sensor with
Au phonon collector
Load inductor
Photon absorber
= Ge/Si island
3 Si/Ge bridges
define link to bath
MMC-based photon detector
Substrate: Ge or Si
2´´ wafer
Energy resolution EFWHM = 3 -10 eV
Rise time R < 50 µs

## Slide 57
To be done: - dry-etching of trenches to define absorber island - recipe already tested:
3 hours of SF6 + O2 (14:1), T = -90 °C, and 500W ICP power
2 wafers without trenches tested in Heidelberg and Saclay
MMC-based photon detector: P1 design

## Slide 58
on etch test wafer
high aspect ratio
MMC-based photon detector: P1 design
To be done: - dry-etching of trenches to define absorber island - recipe already tested:
3 hours of SF6 + O2 (14:1), T = -90 °C, and 500W ICP power
2 wafers without trenches tested in Heidelberg and Saclay

## Slide 59
P1 photon detector in Saclay
X-ray rise time ~ 25-30 µs
Light rise time ~ 250–350 µs
α and muons particles give a different scintillation pulse shape to X-ray pulse
Measurement of the scintillation
time constant

## Slide 60
P1 photon detector in Heidelberg
Copper holder for detectors with trenches
LED light
55Fe calibration source
P1 is 100 times faster than
Ge-NTD based photon sensors
Improve background rejection
Risetime less than 20 µs
 confirmation of Saclay results

## Slide 61
MMC-based phonon sensors
Scintillating Molybdate
Crystal
Photon detector
Phonon collectors: evaporated Au
3 micro-fabricated gold cones:
mechanical support of crystal
thermal contact to sensors
3 AuEr temperature sensors
about 1nJ/K
1-3 independent Nb pickup coils
Energy resolution EFWHM = 50 -100 eV
Rise time R < 200 µs

## Slide 62
Combined photon and phonon detector: P2
copper holder

## Slide 63
Combined photon and phonon detector: P2
copper holder

## Slide 64
Combined photon and phonon detector: P2
copper holder

## Slide 65
Axions couple to photons via the Primakoff effect
I. Irastorza IAXO LoI CERN 2013
Searching for …
AXIONS
AXIONS

## Slide 66
Searching for Axions: Helioscope
Low rate OK for MMC
High QE OK for MMC
Low dark count rate Ok for MMC
Threshold energy OK for MMC
Interantional Axions Observatory : IAXO
- Detector requirements
I. Irastorza IAXO LoI CERN 2013
Microbulk Micromegas @RT

## Slide 67
MMCs @ IAXO
I. Irastorza IAXO LoI CERN 2013
ga = 10-12 GeV-1
4.5 cm
Possibility to be coupled to one of the 8 ports
MOCCA-like detector:
32 readout channel
EFWHM  200 eV
4.5  4.5 cm2
4096 pixels  700 µm position resolution

## Slide 68
MMCs @ IAXO
Possibility to be coupled to one of the 8 ports
About same performance of Micromegas but
different systematics
I. Irastorza IAXO LoI CERN 2013
ga = 10-12 GeV-1
4.5 cm
MOCCA-like detector:
32 readout channel
EFWHM  200 eV
4.5  4.5 cm2
4096 pixels  700 µm position resolution

## Slide 69
MMCs @ IAXO
MOCCA-like detector:
32 readout channel
EFWHM  200 eV
4.5  4.5 cm2
4096 pixels  700 µm position resolution
Possibility to be coupled to one of the 8 ports
About same performance of Micromegas but
different systematics
Detection area large that focused spot
in-situ background measurements
I. Irastorza IAXO LoI CERN 2013
ga = 10-12 GeV-1
4.5 cm

## Slide 70
MMCs @ IAXO
maXs-20 detector:
32 readout channel
EFWHM = 2 eV
2  2 mm2
64 pixels
Allow to investigate fine structures in the spectrum
originating from processes involving electrons,
bremsstrahlung, Compton and axio-recombination
I. Irastorza IAXO LoI CERN 2013
gae = 10-13
2 mm

## Slide 71
Xe gas jet
Xe54+ ions
maXs-200
Experimental Storage Ring at GSI
MMCs on the road to GSI- Darmstadt
Heidelberg University, Friedrich-Schiller University Jena
and Helmholtz-Institute Jena for SPARC
Xe target
H-like Ka1
H-like Ka2
He-like Ka1
He-like Ka2
He-like Kb1,2
H-like Kb1,2
preliminary

## Slide 72
maXs-200
@ 20 mK
atomic ions H+, C+, O+, Ar+
molecular ions N2+, Ar2+, CH3+, Acetone+
… accellerated by 0…150 kV
Creation of lattice defects might spoil energy resolution drastically !
→ first linewidth tests with ions onto maXs-200 detectors at MPI-K
MMCs meet massive particles from CSR at MPIK

## Slide 73: methyl cation CH3+ and its neutral fragments stopped in gold
accellerated CH3+ ions or neutralized CH3
neutral molecule fragments
produced in
dissociative reactions with restgas
All fragments clearly identified by mass (= kinetic energy)
DEFWHM=750eV @ 150keV allows full identification for molecule masses up to 200
MMCs meet massive particles from CSR at MPIK

## Slide 74
MMCs move to the mountains
Modane, France - 15th of September 2015

## Slide 75
….or better under the mountains
Study intrinsic background of MMCs
Test P1 coupled with a scintillating crystals

## Slide 76
metallic magnetic calorimeters
  are versatile low temperature detectors
  high resolution for all kinds of particles
  wide range of energies
  impressive resolving powers in reach
micro-farbrication works
  first detector arrays fabricated
  designed performance is reached
  2d arrays are on the way
multiplexing
  demonstrated principles
Summary and Outlook

## Slide 77
Low temperature physics @KIP
Thank you!

## Slide 78
MMCs @ „ALPS“: Towards sub-eV resolution
Problem: parassitic inductance of bonding wires:
SQUID microstructured on detector chip
Decrease width of meander lines
Insert sensor in SQUID loop

## Slide 79: Cold chemistry @ CSR MPI-K
Junction
…e.g. by observing neutral reaction products
of molecular ions after neutralizing
with an electron in the e-cooler
Study the complex chemistry in cold interstellar clouds
with
O.Novotný, D.W.Savin, C.Krantz, A.Wolf, K.Blaum,
MPI-K Heidelberg, Columbia Astrophysics Lab NY
EFWHM  O(102) eV

## Slide 80
CAbsorber (e-)
CSpin
Signal
Noise
0
1
0
1
Absorber and thermometer are separate systems
Thermalization within the absorber is fast (t < 100ns)
Relaxation time absorber-thermometer finite!
Is there an intrinsic limit?
- Simple model  NO
- Realistic model
E(t) = m(t) B
Energy resolution

## Slide 81
CAbsorber (e-)
CSpin
Signal
Noise
Optimum bandwidth fmax is finite
fmax
0
1
Absorber and thermometer are separate systems
Thermalization within the absorber is fast (t < 100ns)
Relaxation time absorber-thermometer finite!
Is there an intrinsic limit?
- Simple model  NO
- Realistic model  YES
Signal-to-noise is not constant!
E(t) = m(t) B
0
1
Energy resolution

## Slide 82
Energy resolution

## Slide 83
Cabs
fluctuations of energy between sub-systems
(optimum for Cabs = Cspins)
flux noise of SQUID-magnetometer
SF = 2 e L, required:
magnetic Johnson noise
- thermal currents in the metallic components
- marginal in all present detectors
excess noise SF ~ NEr
SF ~ 1/f, Sm|1Hz ≈ 0.023 mEr2/Hz
temperature independent (20mK – 4K)
sensor
SQUID
Cspins
Energy resolution

## Slide 84
QEC determination of 163Ho
Penning Trap mass spectrometry
First experiments at TRIGATRAP (Uni-Mainz) in 2014 *
  Development of efficient Ho ion source using laser ablation
  Uncertainties on 163Dy and 163Ho mass
  reduced by a factor of 2
  Know-how to be applied in SHIPTRAP
In a few months: SHIPTRAP (GSI)
QEC determination within 30 - 100 eV
In a few years: PENTATRAP (MPI-K HD)
QEC determination within 1 eV
*Preparatory studies for a high-precision Penning trap
measurement of the 163Ho electron capture Q-value
F. Schneider et al., submitted to EPJ

## Slide 85
P1 photon detector in Saclay and Heidelberg
      Copper holder developed for detectors with trenches
Saclay
55Fe calibration source
LED light
Coupled to a ZnMoO4 small crystal
Heidelberg
55Fe calibration source
LED light